DEPARTMENT:	WELDING

COURSE:		WELD 028

TITLE:		STRENGTH OF MATERIALS TESTING:	NON-DESTRUCTIVE

WORKSHEET

| Course Objectives (not part of SLO-but derives SLO) | Outcome | Activity | Assessment |
| --- | --- | --- | --- |
| Identify the different methods used to perform non-destructive testing | Students will be able to perform Level I entry level calibrations to magnetic particle, dye penetrant, ultrasonic, and perform visual inspection. | Students will demonstrate the ability to locate weld discontinuities using dye penetrant, magnetic particle, and ultrasonic equipment. | Students will have to pass a visual inspection of their specimen. This will be done by inspecting the weld appearance for weld defects, such as undercut, porosity, and overlap. |
| Demonstrate the proper technique for calibrating the magnetic particle and ultrasonic equipment | Students will demonstrate the ability to locate weld discontinuities using visual inspection, dye penetrant, magnetic particle and ultrasonic testing. | Students will perform calibration of equipment and perform NDT consisting of dye penetrant, magnetic particle and ultrasonic inspection on weld replicas locating surface and subsurface weld discontinuities. | Students will have to pass a written exam on each method as well as specific and practical hands on. |
| Explain each non-destructive method used and when to use a specific method based on the metal characteristics | Students will perform a practical application in non-destructive techniques used in each method. | Students will demonstrate the ability to perform visual inspection along with dye penetrant, magnetic particle, and ultrasonic. | Students will perform visual inspection on weld replicas and write a report explaining what type of weld discontinuities and to what welding code. |

SLO #1	Students will demonstrate the ability to perform Level I entry level calibrations to magnetic particle, dye penetrant, ultrasonic, and perform visual inspection on weldments.

SLO #2	Students will demonstrate the ability to perform visual inspection on weld specimens along with dye penetrant, magnetic particle and ultrasonic examination. Students must also be able to write a clear and concise reports describing what type of weld discontinuity and reference it to a specific welding code.